Casting wall thickness for castability and internal pressure

Index

1. Purpose & Scope	3

2. Definitions	3

3. Thickness calculation	4

3.1. General procedure: description	5

3.2. Thickness calculated by formula (ASME BPVC Section III).	6

4. References	7

# PURPOSE & SCOPE

This procedure establishes the requirements for determining the casting wall thickness of radially split, single-volute, and double-volute single-suction pumps, ensuring both castability and compliance with internal pressure design codes.

This procedure applies to Nova Milanese and La Spezia plants.

# DEFINITIONS

A			Scroll diameter

C.F.		Casting factor

p			Internal design pressure [MPa or psi]

S			Allowable stress [MPa or psi]

Sy			Yield stress at operating temperature [MPa or psi]

Su			Ultimate stress at operating temperature [MPa or psi]

to			Minimum corrosion allowance [mm or in]

t1			Casting wall thickness for castability [mm or in]

t2			Minimum allowable thickness for ASME BPVC Section III, ND3440

topt			Minimum allowable thickness [mm or in]

# THICKNESS CALCULATION

This procedure is based on two main requirements:

- Castability limits.

- Minimum thickness calculated by formula.

| Pump type A | Pump type B |
| --- | --- |

Figure 1: Pump types.

Figure 1 illustrates the geometries considered within this procedure, defining the scroll diameter for both single and double-volute pumps.

The allowable thickness topt  is determined as the greater value betweent1 and t2.

Mod.546 can be used for all the required calculations.

## General procedure: description

Figure 2 presents the minimum casting wall thickness requirements based on manufacturer experience, thereby providing the definition of the minimum wall thickness necessary from a castability perspective t₁.

|  | A [in]; tcast iron [in]; tsteel [in]. 0; 0.3750; 0.2750. 10; 0.5000; 0.4125. 20; 0.6500; 0.5500. 30; 0.7875; 0.6875. 40; 0.9250; 0.8250. 50; 1.0625; 0.9500. 60; 1.2000; 1.1000. |
| --- | --- |

Figure 2: Castability limits.

## Thickness calculated by formula (ASME BPVC Section III).

The minimum required wall thickness t₂ for internal pressure shall be calculated in accordance with the ASME Boiler and Pressure Vessel Code (BPVC), Section III, ND3440.

Figure 3 summarizes the formulas of ASME BPVC Section III for calculating t2.

| Pump type A | Pump type B |
| --- | --- |
| S=C.F.×minSu3.5;Sy1.5 |  |
| t2=maxt,pAS+t0 | t2=maxt,pA2S+t0 |
| C.F. casting factor S allowable stress including casting factor Sy yield stress at operating temperature Su ultimate stress at operating temperature t0 minimum corrosion allowance t2 minimum allowable thickness for ASME BPVC Section III (not less than t) t minimum thickness (6 mm or 0.25 in) |  |

Figure 3: Thickness formulas.

# REFERENCES

ASME Boiler Pressure Vessel Code, Section III, ND3440 Design of specific pump types

Mod.546 – Casting wall thickness for castability and internal pressure

Based on manufacturer experience.

Based on ASME BPVC Section III, ND3440 Design of specific pump types.

The table in S.I. unit is:

| A [mm] | tcast iron [mm] | tsteel [mm] |
| --- | --- | --- |
| 0.00 | 9.53 | 6.99 |
| 254.00 | 12.70 | 10.48 |
| 508.00 | 16.51 | 13.97 |
| 762.00 | 20.00 | 17.46 |
| 1016.00 | 23.50 | 20.96 |
| 1270.00 | 26.99 | 24.13 |
| 1524.00 | 30.48 | 27.94 |

The casting factor is obtainable from:

| Examination | Casting Factor C.F. |
| --- | --- |
| Visual | 0.8 |
| Magnetic particle | 0.85 |
| Penetrant liquid | 0.85 |
| Radiography | 1 |
| Ultrasonic | 1 |
| Magnetic particle/penetrant liquid + ultrasonic/radiography | 1 |